|  | BLOWING AGENTS |  |
| --- | --- | --- |
|  | SYNTHETIC SILICA PRODUCTS, 111/230,HARSH NAGAR, KANPUR Tel. : (0512)-3099938,2554110, Fax No. : 0512-2526257 E-mail: mktg@mlagroup.com, sales@mlagroup.com |  |
|  | Doc. No. : SSP/SPECS/03 | Issue No.: 01 | DATE : 01.07.2005 |  |

Chemical Composition : Azodicarbonamide

Physical Form               : Pale yellow fine powder

PHYSIOCHEMICAL PROPERTIES

| PROPERTES | UNIT | ADC-F2 | ADC-L2 | ADC-EVA | ADC-EV | ADC-PT |
| --- | --- | --- | --- | --- | --- | --- |
| Odor | -- | Odorless | Odorless | Odorless | Odorless | Odorless |
| Average Particle Size | micron | 3-5 | 8-9 | 6-7 | 8-9 | 8-9 |
| pH Value | - | 7.0-7.5 | 7.5-8.0 | 7.5-8.0 | 7.5-8.0 | 7.0-7.5 |
| *Moisture (105ºC, 2 hrs) | % max. | 0.2 | 0.2 | 0.2 | 0.2 | 0.2 |
| Decomposition temperature | ºC | 200(2 | 200(2 | 200(2 | 125(2 | 120(2 |
| Gas composition | -- | N2 & CO | N2 & CO | N2 & CO | N2 & CO | N2 & CO |
| Gas evolution at STP | CC | 225 | 225 | 200 | 120 | 110 |
| Residue on 300 mesh | % max. | Nil | Nil | Nil | 0.5 | 0.5 |
| Packing | Kg/bag | 25 | 25 | 25 | 25 | 25 |

* At the time of packing.

______________________________________________________________________________________________________________________________

This information and our technical advice-whether verbal, in writing or by way of trials are given in good faith but without warranty, and this also applies where proprietary rights of third parties are involved. Our advice does not release you from the obligation to check its validity and to test our products as to their suitability for the intended processes and uses. The application, use and processing of our products and the products manufactured by you on the basis of our technical advice are beyond our control and, therefore, entirely your own responsibility. Our products are sold in accordance with the current version of our General Conditions of Sales and Delivery.

|  | BLOWING AGENTS |  |
| --- | --- | --- |
|  | SYNTHETIC SILICA PRODUCTS, 111/230,HARSH NAGAR, KANPUR Tel. : (0512)-3099938,2554110, Fax No. : 0512-2526257 E-mail: mktg@mlagroup.com, sales@mlagroup.com |  |
|  | Doc. No. : SSP/PDT-SPEC/29 | Issue No.: 01 | DATE : 01.07.2005 |  |

Grade : ADC-EV

Chemical Composition : Azodicarbonamide(Specially treated)

Physical Form               : Pale yellow fine powder

PHYSIOCHEMICAL PROPERTIES

| PROPERTES | UNIT | VALUE |
| --- | --- | --- |
| Odour | -- | Odourless |
| Average Particle Size | micron | 8-9 |
| pH Value | - | 7.5-8.0 |
| *Moisture (105ºC, 2 hrs) | % max. | 0.2 |
| Decomposition temperature | ºC | 125(2 |
| Gas composition | -- | N2 & CO |
| Gas evolution at STP | Cubic Centimeter | 120 |
| Residue on 300 mesh | % max. | 0.5 |
| Packing | Kg/bag | 25 |

* At the time of packing.

______________________________________________________________________________________________________________________________

This information and our technical advice-whether verbal, in writing or by way of trials are given in good faith but without warranty, and this also applies where proprietary rights of third parties are involved. Our advice does not release you from the obligation to check its validity and to test our products as to their suitability for the intended processes and uses. The application, use and processing of our products and the products manufactured by you on the basis of our technical advice are beyond our control and, therefore, entirely your own responsibility. Our products are sold in accordance with the current version of our General Conditions of Sales and Delivery.

|  | BLOWING AGENTS |  |
| --- | --- | --- |
|  | SYNTHETIC SILICA PRODUCTS, 111/230,HARSH NAGAR, KANPUR Tel. : (0512)-3099938,2554110, Fax No. : 0512-2526257 E-mail: mktg@mlagroup.com, sales@mlagroup.com |  |
|  | Doc. No. : SSP/PDT-SPEC/30 | Issue No.: 01 | DATE : 01.07.2005 |  |

Grade : ADC-L2

Chemical Composition : Azodicarbonamide(Specially treated)

Physical Form               : Pale yellow fine powder

PHYSIOCHEMICAL PROPERTIES

| PROPERTES | UNIT | VALUE |
| --- | --- | --- |
| Odour | -- | Odourless |
| Average Particle Size | micron | 8-9 |
| pH Value | - | 7.5-8.0 |
| *Moisture (105ºC, 2 hrs) | % max. | 0.2 |
| Decomposition temperature | ºC | 200(2 |
| Gas composition | -- | N2 & CO |
| Gas evolution at STP | Cubic Centimeter | 225 |
| Residue on 300 mesh | % max. | Nil |
| Solubility | -- | Insoluble in Benzene and water Soluble in Di-methyl formamide |
| Packing | Kg/bag | 25 |

* At the time of packing.

______________________________________________________________________________________________________________________________

This information and our technical advice-whether verbal, in writing or by way of trials are given in good faith but without warranty, and this also applies where proprietary rights of third parties are involved. Our advice does not release you from the obligation to check its validity and to test our products as to their suitability for the intended processes and uses. The application, use and processing of our products and the products manufactured by you on the basis of our technical advice are beyond our control and, therefore, entirely your own responsibility. Our products are sold in accordance with the current version of our General Conditions of Sales and Delivery.

|  | BLOWING AGENTS |  |
| --- | --- | --- |
|  | SYNTHETIC SILICA PRODUCTS, 111/230,HARSH NAGAR, KANPUR Tel. : (0512)-3099938,2554110, Fax No. : 0512-2526257 E-mail: mktg@mlagroup.com, sales@mlagroup.com |  |
|  | Doc. No. : SSP/PDT-SPEC/31 | Issue No.: 01 | DATE : 01.07.2005 |  |

Grade : ADC-EVA

Chemical Composition : Azodicarbonamide (Specially treated)

Physical Form               : Pale yellow fine powder

PHYSIOCHEMICAL PROPERTIES

| PROPERTES | UNIT | VALUE |
| --- | --- | --- |
| Odour | -- | Odourless |
| Average Particle Size | micron | 6-7 |
| pH Value | - | 7.5-8.0 |
| *Moisture (105ºC, 2 hrs) | % max. | 0.2 |
| Decomposition temperature | ºC | 200(2 |
| Gas composition | -- | N2 & CO |
| Gas evolution at STP | Cubic Centimeter | 200 |
| Residue on 300 mesh | % max. | Nil |
| Solubility | -- | Insoluble in Benzene and water Soluble in Di-methyl formamide |
| Packing | Kg/bag | 25 |

* At the time of packing.

______________________________________________________________________________________________________________________________

This information and our technical advice-whether verbal, in writing or by way of trials are given in good faith but without warranty, and this also applies where proprietary rights of third parties are involved. Our advice does not release you from the obligation to check its validity and to test our products as to their suitability for the intended processes and uses. The application, use and processing of our products and the products manufactured by you on the basis of our technical advice are beyond our control and, therefore, entirely your own responsibility. Our products are sold in accordance with the current version of our General Conditions of Sales and Delivery.

|  | BLOWING AGENTS |  |
| --- | --- | --- |
|  | SYNTHETIC SILICA PRODUCTS, 111/230,HARSH NAGAR, KANPUR Tel. : (0512)-3099938,2554110, Fax No. : 0512-2526257 E-mail: mktg@mlagroup.com, sales@mlagroup.com |  |
|  | Doc. No. : SSP/PDT-SPEC/32 | Issue No.: 01 | DATE : 01.07.2005 |  |

Grade : ADC-F2

Chemical Composition : Azodicarbonamide (Specially treated)

Physical Form               : Pale yellow fine powder

PHYSIOCHEMICAL PROPERTIES

| PROPERTES | UNIT | VALUE |
| --- | --- | --- |
| Odour | -- | Odourless |
| Average Particle Size | micron | 3-5 |
| pH Value | - | 7.0-7.5 |
| *Moisture (105ºC, 2 hrs) | % max. | 0.2 |
| Decomposition temperature | ºC | 200(2 |
| Gas composition | -- | N2 & CO |
| Gas evolution at STP | Cubic Centimeter | 225 |
| Residue on 300 mesh | % max. | Nil |
| Solubility | -- | Insoluble in Benzene and water Soluble in Di-methyl formamide |
| Packing | Kg/bag | 25 |

* At the time of packing.

______________________________________________________________________________________________________________________________

This information and our technical advice-whether verbal, in writing or by way of trials are given in good faith but without warranty, and this also applies where proprietary rights of third parties are involved. Our advice does not release you from the obligation to check its validity and to test our products as to their suitability for the intended processes and uses. The application, use and processing of our products and the products manufactured by you on the basis of our technical advice are beyond our control and, therefore, entirely your own responsibility. Our products are sold in accordance with the current version of our General Conditions of Sales and Delivery.

|  | BLOWING AGENTS |  |
| --- | --- | --- |
|  | SYNTHETIC SILICA PRODUCTS, 111/230,HARSH NAGAR, KANPUR Tel. : (0512)-3099938,2554110, Fax No. : 0512-2526257 E-mail: mktg@mlagroup.com, sales@mlagroup.com |  |
|  | Doc. No. : SSP/PDT-SPEC/33 | Issue No.: 01 | DATE : 01.07.2005 |  |

Grade : ADC-4075

Chemical Composition : Azodicarbonamide (Specially treated)

Physical Form               : Pale yellow fine powder

PHYSIOCHEMICAL PROPERTIES

| PROPERTES | UNIT | VALUE |
| --- | --- | --- |
| Odour | -- | Odourless |
| Average Particle Size | micron | 6-7 |
| pH Value | - | 7.0-7.5 |
| *Moisture (105ºC, 2 hrs) | % max. | 0.2 |
| Decomposition temperature | ºC | 191(2 |
| Gas composition | -- | N2 & CO |
| Gas evolution at STP | Cubic Centimeter | 225 |
| Residue on 300 mesh | % max. | Nil |
| Solubility | -- | Insoluble in Benzene and water Soluble in Di-methyl formamide |
| Packing | Kg/bag | 25 |

* At the time of packing.

______________________________________________________________________________________________________________________________

This information and our technical advice-whether verbal, in writing or by way of trials are given in good faith but without warranty, and this also applies where proprietary rights of third parties are involved. Our advice does not release you from the obligation to check its validity and to test our products as to their suitability for the intended processes and uses. The application, use and processing of our products and the products manufactured by you on the basis of our technical advice are beyond our control and, therefore, entirely your own responsibility. Our products are sold in accordance with the current version of our General Conditions of Sales and Delivery.

|  | BLOWING AGENTS |  |
| --- | --- | --- |
|  | SYNTHETIC SILICA PRODUCTS, 111/230,HARSH NAGAR, KANPUR Tel. : (0512)-3099938,2554110, Fax No. : 0512-2526257 E-mail: mktg@mlagroup.com, sales@mlagroup.com |  |
|  | Doc. No. : SSP/PDT-SPEC/34 | Issue No.: 01 | DATE : 01.07.2005 |  |

Grade : ADC-PT

Chemical Composition : Azodicarbonamide (Specially treated)

Physical Form               : Pale yellow fine powder

PHYSIOCHEMICAL PROPERTIES

| PROPERTES | UNIT | VALUE |
| --- | --- | --- |
| Odour | -- | Odourless |
| Average Particle Size | micron | 8-9 |
| pH Value | - | 7.0-7.5 |
| *Moisture (105ºC, 2 hrs) | % max. | 0.2 |
| Decomposition temperature | ºC | 120 |
| Gas composition | -- | N2 & CO |
| Gas evolution at STP | Cubic Centimeter | 110 |
| Residue on 300 mesh | % max. | 0.5 |
| Packing | Kg/bag | 25 |

* At the time of packing.

______________________________________________________________________________________________________________________________

This information and our technical advice-whether verbal, in writing or by way of trials are given in good faith but without warranty, and this also applies where proprietary rights of third parties are involved. Our advice does not release you from the obligation to check its validity and to test our products as to their suitability for the intended processes and uses. The application, use and processing of our products and the products manufactured by you on the basis of our technical advice are beyond our control and, therefore, entirely your own responsibility. Our products are sold in accordance with the current version of our General Conditions of Sales and Delivery.