|  | ONE-PACK PVC STABILIZER | MLA GROUP |
| --- | --- | --- |
|  | UNISTAB - PP |  |
|  | SUMIT CHEMICALS (P) Ltd., 111/230,HARSH NAGAR,KANPUR Tel. : (0512)-2291408-10, Fax No. : 0512-2290057 E-mail : mlgroup123@rediffmail.com, sales@mlagroup.com |  |

UNISTAB-PP is a co-precipitate manufactured under controlled conditions, resulting in a high performance heat stabilizer that is better functionally as well as operationally in PVC processing. It is specially designed for Rigid PVC Pipe application and gives excellent results at low as well as high filler loadings.

###### TYPICAL PHYSIOCHEMICAL PROPERTIES

| PROPERTY | UNIT | PP-2 | PP-3 | PP-4 |
| --- | --- | --- | --- | --- |
| Appearance | -- | Snow White to Cream free flowing Powder |
| Metal Content | % | 30-35 | 35-40 | 50-55 |
| Specific Gravity | -- | 2.2-2.4 | 2.3-2.4 | 2.4-2.5 |
| Moisture | % max | 0.5 | 0.5 | 0.5 |
| pH | -- | 6.5-7.5 | 6.5-7.5 | 6.5-7.5 |
| Melting Point | ºC | 105-110 | 105-110 | 105-110 |
| Residue on 240 mesh | % max | 0.5 | 0.5 | 0.5 |
| Free fatty matter | % max | 0.2 | 0.2 | 0.2 |

1) At the time of packing  2) By IR Moisture Balance 3) IS: 7589-1974 (A-8)   4) IS: 12076-1986(A-2)   5) IS: 2850-1983 (A-5.1)

APPLICATIONS:

- Rigid PVC Pipes : As the filler loading increases the more active heat stabilizer

with more metallics is recommended. PP-2 is recommended for scrap pipes and

very low filler pipes on twin screw. For single screw machines and twin screw

moderate to high filler machines, PP-3 is the optimum grades whereas PP-4 is

recommended for high filler pipes on single screw machine.

This information and our technical advice-whether verbal, in writing or by way of trials are given in good faith but without warranty, and this also applies where proprietary rights of third parties are involved. Our advice does not release you from the obligation to check its validity and to test our products as to their suitability for the intended processes and uses. The application, use and processing of our products and the products manufactured by you on the basis of our technical advice are beyond our control and, therefore, entirely your own responsibility. Our products are sold in accordance with the current version of our General Conditions of Sales and Delivery.