| TYPICAL PHYSIO-CHEMICAL PROPERTIES |  |  |
| --- | --- | --- |
| Property | Unit | Value |
| Surface area (BET) | m²/gm | 200-225 |
| Average Particle Size | Micron | 2.8 |
| pH(2% acqueous solution) | -- | 9.5-10.5 |
| Moisture loss on drying at 105°C( 2 hours) | % | 6.5 |
| lgnition loss at 900°C | % max. | 8.0 |
| Water Absorption | % | 300-440 |
| Bulk Density* | gm/cc | 0.07-0.12 |
| Whiteness | % | 95-98 |
| Refractive Index | -- | 1.47 |
| Specific Gravity | -- | 2.1 |
| Silica (SiO2) | % | 78.5 |
| Calcium (CaO) | % | 19.2 |
| Chlorides | % | Traces |
| Sulphate | % | Traces |
| Lead (pb) | ppm max. | 5 |
| Arsenic (As) | ppm max. | 2 |